COMPANY STANDARD				          PND 01-003.03-15 ML

Vinytol 828 N

Valid from : 1.7. 2015                    					     			    Issue n.:1

This technical data sheet is joined to PND 01 and sets underlying material, characteristics and appropriate particular demands for synthetic leather Vinytol 828 N

| Underlying material | Type | fabric twill-type |
| --- | --- | --- |
|  | Structure | PES/cotton |
| Coating | Composition | PVC |
| Characteristic | Unit | Value | Tested accord to |
| Surface area mass | kg.m-2 | 0,830 ± 0,030 | ČSN 64 7011 |
| Width | cm | 140 ± 3 3 | ČSN 64 7010 |
| Thickness | mm | 1,20 ± 0,10 |  |
| Power at break | lengthways | N/2 cm | 250 | ČSN 64 7012 |
|  | across |  | 140 |  |
| Elongation | lengthways | % | 15 |  |
|  | across |  | 10 |  |
| Resistance to further cracking x/ | lengthways | N | 10 | ČSN 64 7032 |
|  | across |  | 20 |  |
| Cohesion of layers | lengthways | N.m-1 | 500 | ČSN 64 7030 |
|  | across |  | 500 |  |
| Resistance against repeated bend (+ 23 o C) | lengthways | kc/st/st | 5/4/4 | ČSN 64 7029 |
|  | across |  | 5/4/4 |  |
| Abrasion resistance (press 44 kPa, elongation 5%) | dry | c/st./st | 300/4/4 | ČSN 64 7031 |
|  | wet |  | 250/4/4 |  |
| Flammability | most | mm.min-1 | 100 | ČSN ISO 3795 |
| Suitability in the temperature range x/ | o C | -10 to +50 |  |
| Non-tolerant values set in the material data sheet are the guaranteed lowest values x/ specification for informative values Recommended application: haberdashery products |
| Approved for producer: --------------------- ---------------------- date signature and stamp | Approved for customer: --------------------- ---------------------- date signature and stamp |

It substitutes : new						            		Author : Masař